FUMED SILICA IOTA HL7200

Product description

HL7200 is hydrophilic fumed silica with a specific surface area around 200㎡ /g, mainly applied in coatings & paintings, film & UPR, HTV&RTV silicon rubber, adhesives and sealants, printing ink...

| Specification | IOTA HL7200 |
| --- | --- |
| Specific sunface area(BET), ㎡/g | 200±20 |
| pH value in 4% dispersion | 3.9～4.5 |
| Loss on drying(2 hours at 105℃), % | ≤2.0 |
| Loss on ignition(2 hours at 1000℃ based on material dried for 2 hours at 105℃), % | ≤2.0 |
| Sieve Residue(45μm), mg/kg | ≤250 |
| Silica Content(Based on ignited material), % | ≥99.8 |
| Tamped Density(Based on material dried at 105℃ for 2 hours), g/L | 40～60 |

Applications

Coatings & Paintings

Film & UPR

HTV&RTV Silicon Rubber

Adhesives and Sealants

Printing Ink

Fertilizer

Cosmetics

Properties

Reinforcing filler in elastomers

Rheology control and thixotropic agent

Anti-settling,anti-sagging and thickening agent

Free flow aid and anti-caking aid for powders

Package

White kraft paper bag, 10KG/Bag

IOTA CORPORATION LTD.

Add: Sunmoon industry park, 985 Xingzhong Road,Bengbu, China 233000

TeL: 0086-552-3827158   Fax: 0086-552-3822922

Mobile/What's app: 0086-18055290537

WeChat: RachelHo0713

Email: sales04@siliconeoil.net

Website: www.iotasilica.com