## Certificate of Analysis

## IOTA HL 7200 Hydrophilic Fumed Silica

## Batch No.:IOTAHL420020210525HF01

| ITEM |  | Standard | Measured value | Results |
| --- | --- | --- | --- | --- |
| Appearance |  | White powder | White powder | Complied |
| Specific Surface Area(m²/g) |  | 200±20 | 220 | Complied |
| PH Value |  | 3.6-4.5 | 4.08 | Complied |
| Loss on drying, 105℃,% |  | ≤1.5 | 0.68 | Complied |
| Silica Content, % |  | ≥99.8 | 99.84 | Complied |
| Chloride Content% |  | ≤0.025 | 0.001 | Complied |
| Oxide Content, % | Al₂O₃ | ≤0.05 |  | Complied |
|  | TiO₂ | ≤0.03 |  | Complied |
|  | Fe₂O₃ | ≤0.003 |  | Complied |

| Inspector | Yang Jing |
| --- | --- |
| Analysis Time | 2021/05/25 |
| Manufacturing Date | 2021/05/25 |
| Shelf life | 1 years |